PRODUCT DATA SHEET

# Elastic Additive

CRACK BRIDGING PROTECTIVE FOR CONCRETE ADDED ON CEMENT

# PRODUCT DESCRIPTION

Elastic is a one component, elastic additive based on UV-curing acrylic dispersion with excellent crack-bridging properties even at tem- peratures below 0 °C.

Elastic complies with the require- ments of as protective additive

# USES

Elastic is used for protection and en- hancement of concrete structures (normal and light- weight concrete), especially exposed outdoor concrete surfaces with a risk of cracking.

Elastic is used with concrete repair works as an elastic protective coating on smoothing mortar (refer to relevant product / system data sheet), fibre cement and overcoating of existing soundly adhering coatings

- Suitable for protection against,

- Suitable for moisture control

- Suitable for increasing the resistivity

# PRODUCT INFORMATION

CHARACTERISTICS / ADVANTAGES

- Crack-bridging even at low temperatures (-20°C)

- High diffusion resistance against CO2 reducing the rate of carbonation

- Water vapour permeable

- Very good resistance against weathering and ageing

- Environmentally friendly (solvent free)

- Reduced tendency to dirt pick up and contamination

- The system is resistant to aggressive atmospheric in- fluences

# APPROVALS / STANDARDS

Complies with the requirements for Class 0

The product is included in a compilation of tested products and systems as per OS 5a (OS DII)

Determination of dynamic crack bridging properties according to EN 1062-7

Chemical Base	Elastomeric bitumen general adhesive

Appearance / Colour	Milky white

Shelf Life	12 months from date of production if stored properly in undamaged and unopened original sealed packaging.

Storage Conditions	Store in cool and dry conditions. Protect from direct sunlight and frost.

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY

| Density | ~ 1.39 kg/l (at +20°C) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Solid content by weight | ~ 66.1% |  |  |  |  |
| Solid content by volume | ~ 53.4% |  |  |  |  |
| TECHNICAL INFORMATION |  |  |  |  |  |
| Elongation at Break | Elongation at break |  |  |  |  |
|  | - at room temperature (not exposed to weathering): its elongation is 1800% when we add to cement it become 200% |  |  |  |  |
|  | - at -20°C: 70% |  |  |  |  |
| Tensile Adhesion Strength | 2,9 (2,8) N/mm² |  |  | (EN 1542) |  |
| Crack Bridging Ability |  |  |  | (EN 1062-7) |  |
| Freeze Thaw De-Icing Salt Resistance | 2,9 (2,1) N/mm² |  |  | (EN 13687 part 1 & part 2) |  |
| Behaviour after Artificial Weathering | Pass after 2000 hours |  |  | (EN 1062-11) |  |
| Permeability to Water Vapour | Dry film thickness |  | d = 230 µm | (EN ISO 7783-1) |  |
|  | Equivalent air layer thick- ness |  | SD, H2O = 0.35 m | (EN ISO 7783-2) |  |
|  | Diffusion coefficient H2O |  | µH2O = 1,5 x 103 |  |  |
|  | Requirements for breath- |  | ≤ 5 m |  |  |
|  | ability |  |  |  |  |
| Capillary Absorption | w = 0,02 kg/(m²h0.5) |  |  | (EN 1062-3) |  |
| Permeability to CO2 | Dry film thickness |  | d = 160 µm | (EN 1062-6) |  |
|  | Equivalent air layer thick- ness |  | SD, CO2 = 51 m |  |  |
|  | Diffusion coefficient CO2 |  | µCO2 = 3,1 x 105 |  |  |
|  | Requirements for protec- tion |  | SD, CO2 ≥ 50 m |  |  |
| SYSTEM INFORMATION |  |  |  |  |  |

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY

.

Ambient Air Temperature	+8°C min. / +35°C max.

### Relative Air Humidity	< 80%

Dew Point	Temperature must be at least 3°C above dew point.

Substrate Temperature	+8°C min. / +35°C max.

Waiting Time / Overcoating	Waiting time between coats at +20°C substrate temperature:

Curing Treatment	Elastic does not require any special curing but must be protected from rain for at least 4 hours at +20°C.

Applied Product Ready for Use	Full cure: ~ 7 days at +20°C

# APPLICATION INSTRUCTIONS

## SUBSTRATE QUALITY / PRE-TREATMENT

- Elastic Cement is applied to the approved area via caulking gun or trowel. Refer to the SOPREMA SBS Roofing

- Exposed concrete with existing coating:

- Existing coatings must be tested to confirm their ad- hesion to the substrate and their suitability - adhe- sion test average > 0.8 N/mm2 with no single value below 0.5 N/mm2.

- If coating type is unknown, carry out adherence test-

ing to determine which primer is most suitable – wait at least 2 weeks prior to conduct the adhesion test - an average value of 0.8 N/mm² is required with no single value below 0.5 N/mm².

## APPLICATION

- Elastic Cement is applied to the approved area via caulking gun or trowel. Refer to the SOPREMA SBS Roofing

## CLEANING OF TOOLS

Clean all tools and application equipment with clean water immediately after use.

Hardened / cured material can only be removed mechanically.

# LIMITATIONS

Do not apply when there is:

- Expected rain

- Relative humidity > 80%

- Temperature below +8°C and/or below dew point

- Concrete younger than 28 days

Application during cold temperatures below recom- mended application temperatures may reduce adhe- sion values.

Elastic is not a chemical resistant coating

Dark colour shades (especially black, dark red and blue, etc.) may fade more rapidly than other lighter tone colours. A refreshing coat might be required at an earlier interval than usual.

Where colour fade may occur the protective proper- ties of the coating will remain unaffected

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY

# VALUE BASE

All technical data stated in this Product Data Sheet are based on laboratory tests. Actual measured data may vary due to circumstances beyond our control.

# LOCAL RESTRICTIONS

Please note that as a result of specific local regulations the performance of this product may vary from coun- try to country. Please consult the local Product Data Sheet for the exact description of the application fields.

# ECOLOGY, HEALTH AND SAFETY

For information and advice on the safe handling, stor- age and disposal of chemical products, users shall refer to the most recent Safety Data Sheet (SDS) con- taining physical, ecological, toxicological and other safety-related data.

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY