PRODUCT DATA SHEET

# Epoxy Coal Tar

Heavy duty Epoxy tar based epoxy protective coating for concrete

# DESCRIPTION

Epoxy Tar is a two part reaction harden- ing, chemical resistant coating based on coal tar epoxy resin, in combination with mineral fillers Made From Cashew oil its safe to be used in fridges and food health industries.

DIMAPCHEM CT is based on a solvent based Epoxy Resin system modified with a hydrocarbon resin, derived from coal tar. This modified tar is free from pitch and hence represents a low hazard during use. i.e. DIMAPCHEM CT is much more user friendly than conventional Pitch Epoxy Coatings. DIMAPCHEM CT is supplied as a two pack material in pre weighed quantities ready for mixing and use.

# USES

Dimapchem Coal Tar is used as a protective chem- ical resistant coating for concrete, as internal and ex- ternal coating for buried and submerged structures in wastewater, seawater or highly aggressive soils such as:

- Sewage, effluent or waste treatment plants

- Immersed piers

- Concrete silos

- Ship hulls, pipelines, cooling towers

- Oil catchment tanks, pipes and piles of off-shore platforms

- Structures immersed in fresh and salt water

- Chemical storages

- Marine structures

- Fridges food industries

# PRODUCT INFORMATION

CHARACTERISTICS / ADVANTAGES

- Tough hard, heavy duty

- Abrasion and impact resistant

- Excellent resistance to water and chemicals

- Resistant to microbes

- Hold temperature up to -30o

- Made From Cashew oil its safe to be used in fridges and food health industries.

Product declaration	Confirms to IS 14948 : 2001

Chemical base	Epoxy resin modified with coal tar

Shelf life	12 months from date of production

Storage conditions	The product must be stored in original, unopened and undamaged sealed

packaging in dry conditions at temperatures between +5 °C and +35 °C.

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY

Appearance / Colour	Part A+B	all colors available

Part A		 Part B

Density	~1.65 kg/L (Part A+B mixed, +30 °C)	(EN ISO 2811-1)

Flash point	> 30 °C	(ASTM D93)

### Solid content by weight	~85 %

Solid content by volume	~75 %	(IS 101 Part 8/Sec 6)

# TECHNICAL INFORMATION

Shore A hardness	~90	(ASTM D2240)

Resistance to impact	No signs of cracking, flaking or detachment from the panel or

loss of adhesion between coats when tested on abrasive blas- ted panel (7 days, 2 m height)

### Tensile adhesion strength	Substrate	 Tensile adhesion strength

(IS 101

Part 5/Sec 3)

(EN 1542)

Concrete

Steel

| Chemical resistance | Chemicals |  | 24 hours |  | 3 days |  | 7 days (IS 4631-1968) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sea water |  | A |  | A |  | A |
|  | Water |  | A |  | A |  | A |
|  | Nitric acid 1 % |  | A |  | D |  | D |
|  | Hydrochloric acid 1 % |  | A |  | D |  | D |
|  | Sulphuric acid 1 % |  | A |  | D |  | D |
|  | Diesel |  | A |  | A |  | A |
|  | NaOH 1 % |  | A |  | A |  | A |

# SYSTEM INFORMATION

A = resistant, D = resistant but with discolouration and/or loss of gloss, C = not resistant

Test temperature: +30 °C

Dry film thickness	~125 microns per coat

# APPLICATION INFORMATION

Mixing ratio	Part A : Part B = 16 : 84 (by weight)

These figures are theoretical and do not allow for any additional material due to surface porosity, surface profile, variations in level and wastage etc.

Ambient air temperature	Maximum	 +30 °C

Minimum	 +10 °C

Relative air humidity	Maximum	 75 %

Dew point	Beware of condensation.

The substrate must be at least +3 °C above the dew point to reduce the risk of condensation, which may lead to adhesion failure of final finish. Be aware that the substrate temperature may be lower than the ambient temperature.

Substrate temperature	Maximum	 +30 °C

Minimum	 -30 °C

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY

### Substrate moisture content	≤ 4 %

Pot life	~2 hours at +30 °C

Curing time	Full cure in ~7 days at +30 °C

Note: Times are approximate and will be affected by changing ambient conditions.

Gel time	~24 hours max.

### Waiting time / Overcoating	Substrate temperature	Minimum	Maximum

+10 °C	16 hours	7 days

+20 °C	8 hours	7 days

+30 °C	4 hours	7 days

Note: The waiting times between applications depend largely on temperat- ure and weather. Lower temperature will increase the minimum and the maximum time specified. To ensure good intercoat adhesion, light grinding of the previous coat followed by a thorough de-dusting is required.

Drying time	Surface dry	 ~1.5 h	 (IS 101 Part 3/Sec 1)

Hard dry	 ~12 h

# BASIS OF PRODUCT DATA

All technical data stated in this Product Data Sheet are based on laboratory tests. Actual measured data may vary due to circumstances beyond our control.

# ECOLOGY, HEALTH AND SAFETY

User must read the most recent corresponding Safety Data Sheets (SDS) before using any products. The SDS provides information and advice on the safe handling, storage and disposal of chemical products and con- tains physical, ecological, toxicological and other safety-related data.

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY

# APPLICATION INSTRUCTIONS

## EQUIPMENT

### Mixing

Low speed electric single paddle mixer (300–400 rpm) or other suitable equipment.

### Application

- Brush application: Distemper brushes, round brushes or radiator brushes

- Roller application: Short pile lamb skin roller

## SUBSTRATE QUALITY

- The concrete substrate must be sound and of suffi- cient compressive strength (minimum 25 N/mm2) with a minimum pull off strength of 1.5 N/mm2.

- The substrate must be clean, dry and free of all con-

taminants such as dirt, oil, grease, coatings and sur- face treatments, etc. If in doubt apply a test area first.

- Weak concrete must be removed and surface defects

such as blowholes and voids must be fully exposed.

- The concrete or screed substrate has to be primed or levelled in order to achieve an even surface.

## SUBSTRATE PREPARATION

- Concrete substrates must be prepared mechanically using grinding, wire-brushing, abrading, scarifying or preferably by high pressure water/sand blasting equipment to remove cement laitance and achieve an open textured surface.

- Weak concrete must be removed and surface defects

such as blow holes, cavities, pinholes and voids must be fully exposed.

- Repairs to the substrate, filling of blowholes/voids

and surface levelling must be carried out using ap- propriate. High spots can be re- moved by grinding.

- All dust, loose and friable material must be com-

pletely removed from all surfaces before application of the product, preferably by brush and/or vacuum.

## MIXING

- Stir Part B thoroughly to remix any settled part.

- Add Part A and mix thoroughly with an electric single paddle mixer for 3 minutes until a uniform mix has been achieved.

## APPLICATION

IMPORTANT

Do not apply Coal Tar on substrates with rising moisture.

IMPORTANT

Freshly applied must be protected from damp, con- densation and water for at least 24 hours.

1. Apply to concrete or steel surface using airless spray, conventional spray, brush and/or roller. A minimum of 2 coats must be applied.

## CLEANING OF TOOLS

Clean all tools and application equipment with Cleaner immediately after use. Hardened or cured material can only be mechanically removed.

# LOCAL RESTRICTIONS

Note that as a result of specific local regulations the declared data and recommended uses for this product may vary from country to country. Consult the local Product Data Sheet for exact product data and uses.

Visit us on : http://www.dimapchem.com/

EMAIL: Info@dimapchem.com

ALL PRODUCTS EXAMINED BY GFC LAB-ITALY